## Slide 1: 电池全生命周期健康管理系统
结题汇报
Jun. 7，2024
小组成员：王浩羽、李宗润、徐 涵
指导老师：卢周广、高 源、宋 轩
企业导师：袁 飞

## Slide 2: Background
Advantage：
Improve battery performance and safety
Provides support for the secondary utilization of batteries
2 / 45
Notes: 背景和意义的阐述需要清晰的说明项目的why的内容！为什么我们要做这个项目，基于哪些背景需求，解决了这些需求有什么意义，这些意义才是我们科研工作的研究价值。

## Slide 3: Background
材料科学与工程系
李宗润
计算机科学与工程系
王浩羽
深港微电子学院
徐涵
3 / 45
Notes: 背景和意义的阐述需要清晰的说明项目的why的内容！为什么我们要做这个项目，基于哪些背景需求，解决了这些需求有什么意义，这些意义才是我们科研工作的研究价值。

## Slide 4
Test platform
Test process
Cycle and EIS test
李宗润
Part A: Materials Science
and Engineering

## Slide 5: Test platform
Test platform:
  Electrochemical Workstation
  EIS test platform
Battery：
  SANYO&PANA (4.3V)
  18650 (4.3V)
  Button battery: LIR2032 (3.6V)
5 / 45
Electrochemical Workstation
ElS Test Channel
Control Panel

## Slide 6: EIS test
EC-LAB
BTSDA
6 / 45

## Slide 7: Test process
CC
CV
Rest
EIS Test
Discharge
Record
10 cycles
Record
7 / 45

## Slide 8: Test process
Data relativity in specific test time：
EIS Measurement States
Data source: Identifying degradation patterns of lithium ion batteries from impedance spectroscopy using machine learning
https://zenodo.org/records/3633835
Fitting Results
8 / 45

## Slide 9
Hardware System Design
Data Collect
Data Processing
Compare and Analysis
徐涵
Part B:
Microelectronics

## Slide 10: Hardware System Design
Objective: To measure the complete charge and discharge curve of the battery
Work: Set up the hardware circuit to charge and discharge the battery and sample the voltage and current
Voltage monitor：ADS1115
Current monitor：INA226
Battery charging：PW4035
Serial port communciation：CH340
Storage module：W25Q64
10 / 45

## Slide 11: Schematic
Voltage monitor
ADS1115
range：6.144V
LSB：187.5uV
Cuttent monitor：INA226
range：3.2A
LSB：0.1mA
Battery charging：
PW4035
MAX current up to2A
constant current and constant voltage
11 / 45

## Slide 12: PCB
1：W25Q64
2：ADS1115
3：INA226
4：PW4035
1：PW4035
2：INA226
3: ADS1115
4：W25Q64
5：STM32
1：PCB
2：STLINK
3: CH340
4：Battert
5：electronic device
PCB
Real part
Test
12 / 45

## Slide 13: Data Collect
discharge voltage
discharge curve
2A discharge
charge curve
discharge current
charge voltage
charge current
13 / 45

## Slide 14: Date processing
discharge--EIS
discharge
impedance Z：
dZ：
；
DRT：
EIS
exponential decay
14 / 45

## Slide 15: 数据处理
discharge--EIS
0.001S sample frequency
50S sample time
Z：
Z
dZ
DRT
EIS
red: real EIS
blue: calculated EIS
15 / 45

## Slide 16: reverse：DRT→EIS
EIS（EIS-DRT-EIS）
EIS（device）
DRT-tools[1]
DRT
similarity ：
EIS and EIS（from DRT）
calculation correct
16 / 45

## Slide 17: reverse：dZ→DRT
DRT（from EIS）
DRT（DRT-dZ-DRT）
dZ
similarity ：
DRT and DRT（from dZ）
calculation correct
17 / 45

## Slide 18: Compare and Analysis
Z（compare）
red: Z
blue: reverse Z
Battery
EIS
correct calculation but incorrect EIS
EIS change on various SOC
Battery cell not enough
Sample frequency not enough（1KHZ vs1MHZ）
18 / 45

## Slide 19
Goals and Objectives
Proposed Methods
Experimental Results
Conclusion
System Demo
王浩羽
Part C: Computer Science
and Engineering

## Slide 20: Goals and Objectives
Charging Curve
EIS Profile
Capacity Degradation Curve
Estimate
Predict
Remaining Useful Life (RUL)
20 / 45
Notes: 我们的目标是通过充放电曲线和EIS曲线两类电池数据，预测电池当前容量，并结合容量历史数据，进一步估计电池的剩余使用寿命RUL

## Slide 21: Proposed Methods
Step2
Predict Current Capacity
Calculate State of Health
(SOH)
Step1
Data Processing
Step3
Estimate
Remaining Useful Life
(RUL)
21 / 45
Notes: 可以看到，我们提出的方法共有三个步骤，步骤一为数据预处理，分布提取出充电曲线中电压和电流特征以及EIS曲线中实部和虚部特征，进而构成一个特征向量输入到第二步的DNN中获得预测的容量，也就是SOH，结合历史数据通过时间窗口线性回归模型，估计出RUL。

## Slide 22: Proposed Methods
Step2: CapaDeepNet
Deep Neural Net for Battery Capacity Prediction
 | layer | in-dim | out-dim
1 | FC | Feature-size | 32
2 | FC | 32 | 64
3 | FC | 64 | 72
4 | FC | 72 | 128
5 | FC | 128 | 64
6 | FC | 64 | 64
7 | FC | 64 | 32
8 | FC | 32 | 16
9 | FC | 16 | 8
10 | FC | 8 | 1
DeepNet Structure:
Hyper Params:
Epoch：50
Batch Size：16
22 / 45
Notes: 这是我们的CapaDNN模型，由十个MLP层构成，超参设置如上

## Slide 23: Dataset 1: 18650
Dataset 1 (Self-measuring):
6 Batteries of “18650”
battery | charging protocol | CC current | CV voltage | cycle
1 | CC-CV | 2.0A | 4.2V | 859
2 | CC-CV | 2.0A | 4.2V | 869
3 | CC-CV | 2.0A | 4.2V | 900
4 | CC-CV | 3.0A | 4.2V | 894
5 | CC-CV | 3.0A | 4.2V | 844
6 | CC-CV | 3.0A | 4.2V | 920
23 / 45
Notes: 我们的第一个数据集称之为18650，由六块18650电池构成，他们被分为两组，按照恒流充电的不同。前三块2.0A，后三块3.0A

## Slide 24: Dataset 1: 18650
EIS Profiles:
Can NOT Use due to
the INSTRUMENTs
24 / 45
Notes: 虽然我们也测量了该数据集的EIS，但是由于仪器问题，曲线杂乱无章，无法使用

## Slide 25: Dataset 1: 18650
Data in Dataset (Battery 1):
Only Charging Curve
Battery Charging Curves
(1 cycle)
Capacity Degradation Curve
25 / 45
Notes: 那么我们只能用它的充电曲线进行实验，右图为它的容量下降曲线

## Slide 26: Dataset 1: 18650
Step1: Data Processing
CV Current
CC Voltage
CC
Voltage
CV Current
Range
CC -> U: 4.0 ~ 4.2V
CV -> I: 2.0 ~ 0.5A
Sample points number
CC Voltage: 20
CV Current: 10
26 / 45
Notes: 第一步，数据预处理，首先看上面两幅图，我们分别截取了CC部分的电压4.0-4.2V，和CV部分电流2.0A-0.5A，然后将截取区域全部绘制在一张图上得到下图。可以看到从白色到深蓝色是相当有规律的，这位后面的训练打下一个很好的基础。

## Slide 27: Dataset 1: 18650 – Capacity Prediction
Step2: CapaDeepNet
Battery 1: Training Data
(training and validation)
Battery 2 and 3: Evaluation
27 / 45
Notes: 第一组实验结果，其中，我们使用电池1作为训练集，当然它本身也进一步分割为训练和测试两部分。电池2和3不参与训练，只作为测试集衡量模型性能。可以从拟合结果中看到，结果非常的好，最大平均相对误差不超过1%

## Slide 28: Dataset 1: 18650 – Capacity Prediction
Step2: CapaDeepNet
Battery 4: Training Data
(training and validation)
Battery 5 and 6: Evaluation
28 / 45
Notes: 第二组同理，电池6虽然平均相对误差超过了1%，但是这也是由于尾部拟合不够好的原因造成的，由图中也可以看出

## Slide 29: Dataset 1: 18650 – RUL Estimation
Step3: Time-window Linear Regression
Battery 1
Battery 2
Battery 3
440-540 cycles
540-640 cycles
Time-window
29 / 45
Notes: 这是时间窗口线性回归模型，我们展示了440-540，540-640这两组时间窗口，可以观察到在容量下降的后半部分，它保持了比较好的线性性

## Slide 30: Dataset 1: 18650 – RUL Estimation
Step3: Time-window Linear Regression
Battery 4
Battery 5
Battery 6
460-560 cycles
520-620 cycles
Time-window
30 / 45

## Slide 31: Dataset 2: 3633835
Choose Battery: 25C05
(from 8 batteries)
Choose state V
Open-source; EIS Only
I
II
III
IV
V
VI
IX
Data source: Identifying degradation patterns of lithium ion batteries from impedance spectroscopy using machine learning
https://zenodo.org/records/3633835
https://zenodo.org/records/3633835
31 / 45
Notes: 第二个数据集，3633835，它是一个开源数据集，我们选择了电池25C05开展实验，它包含多个state的EIS，我们选取V，原因是其他很多EIS没有规律，只有1，5，6具有较好的可解释性，原论文选用了V，因此我们也使用V进行进一步研究

## Slide 32: Dataset 2: 3633835 – Capacity Prediction (Interval)
Choose Battery: 25C05
EIS Features (Method 1): Interval of Re/Im Segments
EIS Features
(for all cycles)
32 / 45
Notes: 那么这是我们截取的EIS的实部和虚部，所有cycle均绘制在图上

## Slide 33: Dataset 2: 3633835 – Capacity Prediction (Interval)
Step2: CapaDNN
Capacity Degradation Curve
Prediction results
33 / 45
Notes: 可以看到，数据集中给出了较多的循环周期，但是红线之后的数据我们并不关心。预测结果很好

## Slide 34: Dataset 2: 3633835 – Capacity Prediction (Characters)
Choose Battery: 25C05
EIS Features (Method 2): EIS Characters
EIS Characters
(for 1 cycle)
EIS Features
(for all cycles)
34 / 45
Notes: 我们使用了另一种方法去完成这项任务，分别选取一条EIS曲线的峰值、谷值、欧姆阻抗、频率0.1处以及过零点的直线与曲线切点，将它们的实部、虚部、以及两者平方和开根号提取出来绘制在右图中。可以看到，变化具有高度的规律性。
（欧姆阻抗当然虚部肯定是0，平方和开根号也等于实部，简单起见我也没处理俩东西）

## Slide 35: Dataset 2: 3633835 – Capacity Prediction (Characters)
Step2: CapaDNN
Capacity Degradation Curve
Prediction results
0.4308
0.91%
0.3170
0.78%
35 / 45
Notes: 拟合结果如图，发现平均相对误差只有0.78%

## Slide 36: Dataset 2: 3633835 – Comparison
Step2: CapaDNN:
Method1: Interval
Method2: Characters
Mean Relative Error:
1.23% =====>>>>>> 0.78%
36 / 45
Notes: 第二种方法，在选取了更少的数据点的情况下，获得了比方法一更好的结果，这体现了特征提取的有效性

## Slide 37: Dataset 2: 3633835 – RUL Estimation
Step 3:
Time-window Linear Regression
40–60 cycles
50–70 cycles
60–80 cycles
70–90 cycles
Model shows a poor Robustness!
37 / 45
Notes: RUL估计结果，我们发现从2.62%到9%以上，结果变化剧烈，这意味现在的模型在鲁棒性上表现较差

## Slide 38: Dataset 3: Button Cell
Self-measuring
Single Battery Only
Capacity Degradation Curve
EIS Profile
38 / 45
Notes: 纽扣电池数据集包含一块纽扣电池，它的特点是同时具有EIS曲线和充放电曲线

## Slide 39: Dataset 3: Button Cell
Features
EIS Features
(for all cycles)
Charging Curve
Features
(for all cycles)
39 / 45
Notes: 上图和下图分别是我们提取到的充电曲线和EIS曲线

## Slide 40: Dataset 3: Button Cell - Results
Step2: CapaDNN
Step 3: Time-window Linear Regression
40 / 45
Notes: 容量预测结果在左侧，平均相对误差只有0.24%，相当不错了。右边是RUL回归结果，同样有鲁棒性较差的问题

## Slide 41: Dataset 4: NASA (Deprecated)
EIS Profiles for Several Batteries
Totally Ridiculous!
41 / 45
Notes: 我们同样探索了市面上其他开源数据集，但是并没有很大同时具有充放电和EIS曲线的开源数据集，如NASA的EIS完全无法使用

## Slide 42: Conclusion
To enhance the Accuracy and Applicability of our model,
For CapaDNN:
Good enough for LAB datasets
Collect more realistic data from REAL USAGE
For Time-window Linear Regression:
Effective for some cases
Poor Robustness
Sensitive to Abnormal value
42 / 45
Notes: 结论：纯念PPT就行

## Slide 43: System Demo
Demo Web
43 / 45

## Slide 44: Reference
1．Wang, S., Jin, S., Bai, D., Fan, Y., Shi, H., & Fernandez, C. (2021). A critical review of improved deep learning methods for the remaining useful life prediction of lithium-ion batteries. Energy Reports, 7, 5562–5574. https://doi.org/10.1016/j.egyr.2021.08.182
2．Ansari, S., Ayob, A., Hossain Lipu, M. S., Hussain, A., & Saad, M. H. M. (2022). Remaining useful life prediction for lithium-ion battery storage system: A comprehensive review of methods, key factors, issues and future outlook. Energy Reports, 8, 12153–12185. https://doi.org/10.1016/j.egyr.2022.09.043
3．Wang, S., Jin, S., Deng, D., & Fernandez, C. (2021). A Critical Review of Online Battery Remaining Useful Lifetime Prediction Methods. Frontiers in Mechanical Engineering, 7. https://doi.org/10.3389/fmech.2021.719718
4．Park, K., Choi, Y., Choi, W. J., Ryu, H.-Y., & Kim, H. (2020). LSTM-Based Battery Remaining Useful Life Prediction With Multi-Channel Charging Profiles. IEEE Access, 8, 20786–20798. https://doi.org/10.1109/access.2020.2968939
5．Xu, Q., Wu, M., Khoo, E., Chen, Z., & Li, X. (2023). A Hybrid Ensemble Deep Learning Approach for Early Prediction of Battery Remaining Useful Life. IEEE/CAA Journal of Automatica Sinica, 10(1), 177–187.
https://doi.org/10.1109/jas.2023.123024
6．Lu, J., Xiong, R., Tian, J., Wang, C., & Sun, F. (2023). Deep learning to estimate lithium-ion battery state of health without additional degradation experiments. Nature Communications, 14(1). https://doi.org/10.1038/s41467-023-38458-w
7．Zhang, Y., Tang, Q., Zhang, Y., Wang, J., Stimming, U., & Lee, A. A. (2020). Identifying degradation patterns of lithium ion batteries from impedance spectroscopy using machine learning. Nature Communications, 11(1). https://doi.org/10.1038/s41467-020-15235-7

## Slide 45: 谢谢大家！ 请各位老师批评指正！

## Slide 46
3633835 dataset
Capacity Degradation Curves
For 8 Batteries
Appendix: